M92 CRYSTAL PARTITION

Modules

Product files

| ### MODULE A | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module A: totally blind. Standard module width: 1,200 mm. Total thickness: 80 mm. Made with Sendzimir galvanised-steel inner and outer frames per European standard EN10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester powder and polymerised at 200ºC. Total paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Interior insulation with 50-mm thick, 30 Kg/m3 dense mineral wool. 13-mm fibreboard panels coated with 0.3-mm vinyl laminate with 2-mm edging. Panels and frames with 10-mm grooves thanks to splice joints clipped to structure. Acoustic insulation: 41.5 dB per UNE 74040. Reinstallation and interchangeability of modules. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE D Glazed | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module D: totally glazed. 3,600-mm wide (as maximum) between axes with 1,200-mm wide panes, 10- or 12-mm thick (to choose), joined by Polymethyl methacrylate PMMA flush joints. Total partition thickness: 80 mm. Made with Sendzimir galvanised-steel perimeter frames per European standard EN 10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. The levelled panes are 5+5 or 6+6 mm (to choose) joined by a sheet of PVB. Levelled horizontal frames mitred with the vertical frames which form 10-mm grooves thanks to splice joints secured to the structure. The panes can be demounted from the structure independently thanks to perimeter frames on each side of the pane. Module reinstallation and interchangeability. Module reinstallation and interchangeability. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE D Glazed | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module D: totally glazed. 1,200-mm wide between axes with one 1,200-mm wide pane, 8-, 10- or 12-mm thick (to choose), joined by Polymethyl methacrylate PMMA flush joints. Total partition thickness: 80 mm. Made with Sendzimir galvanised-steel perimeter frames per European standard EN 10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. The levelled panes are 4+4, 5+5 or 6+6 mm (to choose) joined by a sheet of PVB. Levelled horizontal frames mitred with the vertical frames which form 10-mm grooves thanks to splice joints secured to the structure. The panes can be demounted from the structure independently thanks to perimeter frames on each side of the pane. Module reinstallation and interchangeability. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE D Glazed | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module D: totally glazed. 2,400-mm. wide between axes with two 1,200-mm. wide panes, 8-, 10- or 12-mm. thick (to choose), joined by Polymethyl methacrylate PMMA flush joints. Total partition thickness: 80 mm. Made with Sendzimir galvanised-steel perimeter frames per European standard EN 10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. The panes are 4+4, 5+5 or 6+6 mm (to choose) joined by a sheet of PVB. Levelled horizontal frames and mitred joints to the vertical frames which form 10-mm grooves thanks to splice joints secured to the structure. The panes can be demounted from the structure independently thanks to perimeter frames on each side of the pane. Module reinstallation and interchangeability. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE D Glazed | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module D: totally glazed. Unlimited-length sections with more than three, as required, 1,200-mm wide panes, 12-mm thick, joined by Polymethyl methacrylate PMMA overlap joints. Total partition thickness: 80 mm. Made with Sendzimir galvanised-steel perimeter frames per European standard EN 10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. The panes are 6+6 mm joined by a sheet of PVB. Levelled horizontal frames mitred with the vertical frames which form 10-mm grooves thanks to splice joints secured to the structure. The panes can be demounted from the structure independently thanks to perimeter frames on each side of the glass. Module reinstallation and interchangeability. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Door | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module G: glazed, floor-to-ceiling door, 909-mm wide between axes. Total partition thickness: 80 mm. Made with Sendzimir galvanised-steel perimeter frames per European standard EN 10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 10-mm thick, 830-mm wide, Clarit tempered-glass door leaf, with matching hinges and latch. The frames form 10-mm grooves thanks to splice joints secured to the structure. Module reinstallation and interchangeability. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Door | M2. Supply and installation of Dynamobel M92 Crystal demountable partition with hidden profiling, module W: glazed, floor-to-ceiling, double-leaf door, 1,742-mm wide between axes. Total partition thickness: 80 mm. Made with Sendzimir galvanised-steel perimeter frames per European standard EN 10.142-A1:1994. (DX51D+Z). Previously degreased, visible metal components, electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Two 10-mm thick, 830-mm wide, Clarit tempered-glass door leaves, with matching hinges and latch. The frames form 10-mm grooves thanks to splice joints secured to the structure. Module reinstallation and interchangeability. Quality assurance UNE EN ISO 9002 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |