1:10

DEMOUNTABLE PARTITION

Descriptive memories

| ### MODULE A | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module A: totally blind. Standard module width: 1,200 mm. Total thickness: 100 mm. Made with Sendzimir galvanised-steel frame per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module B: mixed central-glass section (blind to 915 mm and glazed to 2,120 mm). Central glass section may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces (either the panels or an aluminium profile). Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B blind | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module B blind: totally blind, divided in 3 panels (grooves at 917.5 and 2117.5 mm). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting frame in Sendzimir galvanised steel per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B inverted | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module B inverted: mixed central-bind section (glazed to 915 mm and blind to 2,120 mm). Upper and lower glass sections may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces (either the panels or an aluminium profile). Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B glazed | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module B glazed: totally glazed, divided in 3 panes (grooves at 917.5 and 2117.5 mm). It may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. The horizontal grooves between panes are 5 mm wide and 16 mm deep. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B+F | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module B+F: mixed central and upper glass sections (blind to 915 mm and glazed to ceiling, with a groove at 2,117.5 mm). Central and upper glass sections may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces (either the panels or an aluminium profile). Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE C | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module C: mixed lower-glass section (glazed to 2,120 mm and blind to ceiling). Lower glass section may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces (either the panels or an aluminium profile). Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE C+F | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module C+F: totally glazed, divided in 2 panes (groove at 2,117.5 mm). It may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. The horizontal grooves between panes are 5 mm wide and 16 mm deep. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE D | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module D: totally glazed. It may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE E | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module E: mixed upper-glass section (blind to 915 mm and blind to ceiling). Upper glass section may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces (either the panels or an aluminium profile). Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE E blind | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module E: totally blind, divided in 2 panels (groove at 917.5 mm). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting frame in Sendzimir galvanised steel per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE F | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module F: mixed upper-glass section (blind to 2,115 mm and blind to ceiling). Upper glass section may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces (either the panels or an aluminium profile). Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE F blind | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module F blind: totally blind, divided in 2 panels (groove at 2,117.5 mm). Standard module width: 1,200 mm. Total thickness: 100 mm. Made with a self-supporting frame in Sendzimir galvanised steel per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Upper and bottom runners are 53mm-thick and leave 20mm to the floor and the ceiling. Interior insulation with 68-mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module G: blind door with floor-to-ceiling door jambs. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling lightweight door leaf made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. Door leaf is 910 mm wide and 100 mm thick or 914 mm wide and 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module G: double-glazed door with floor-to-ceiling door jambs. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling double-glazed door leaf, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles, which is 910 mm wide and 100 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module G: single-glazed door with floor-to-ceiling door jambs. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling single-glazed door leaf, with an 8mm-thick tempered glass pane framed by painted aluminium profiles, which is 914 mm wide and 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module G: glazed door with floor-to-ceiling door jambs. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling tempered glazed Clarit door leaf; which is 914 mm wide and 10 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module K: blind door with blind top panel. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Lightweight door leaf made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. Door leaf is 910x2,017x100 mm or 914x2,017x50 mm. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module K: double-glazed door with blind top panel. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Double-glazed door leaf, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles; which is 910 mm wide, 100 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module K: single-glazed door with blind top panel. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Single-glazed door leaf, with an 8mm-thick tempered glass pane framed by painted aluminium profiles; which is 914 mm wide, 50 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module K: glazed door with blind top panel. Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Tempered glazed Clarit door leaf; which is 914 mm wide, 10 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module P: blind door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Lightweight door leaf made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. Door leaf is 910x2,017x100 mm or 914x2,017x50 mm. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module P: double-glazed door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Double-glazed door leaf, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles; which is 910 mm wide, 100 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module P: single-glazed door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Single-glazed door leaf, with an 8mm-thick tempered glass pane framed by painted aluminium profiles; which is 914 mm wide, 50 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module P: glazed door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,004 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Tempered glazed Clarit door leaf; which is 914 mm wide, 10 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module S: blind double door with blind top panel. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Lightweight door leaves made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. Door leaves are 910x2,017x100 mm or 914x2,017x50 mm. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module S: double-glazed double door with blind top panel. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Double-glazed door leaves, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles; which are 910 mm wide, 100 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module S: single-glazed double door with blind top panel. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Single-glazed door leaves, with an 8mm-thick tempered glass pane framed by painted aluminium profiles; which are 914 mm wide, 50 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module S: glazed double door with blind top panel. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 16mm-thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. The grooves the modulation features are 5 mm wide and 16 mm deep, and the panels close over a 1mm-thick PVC joint which provides sound insulation. Interior insulation with 50/60-mm thick, 30/40 Kg/m3 dense mineral fibre. Tempered glazed Clarit door leaves; which are 914 mm wide, 10 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module W: blind double door with floor-to-ceiling door jambs. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling lightweight door leaves made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. Door leaves are 910 mm wide and 100 mm thick or 914 mm wide and 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module W: double-glazed double door with floor-to-ceiling door jambs. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling double-glazed door leaves, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles, which are 910 mm wide and 100 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module W: single-glazed double door with floor-to-ceiling door jambs. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling single-glazed door leaves, with an 8mm-thick tempered glass pane framed by painted aluminium profiles, which are 914 mm wide and 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module W: glazed double door with floor-to-ceiling door jambs. Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling tempered glazed Clarit door leaves; which are 914 mm wide and 10 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE X Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module X: blind double door with lock leaf and inactive leaf, with stiles to ceiling. Variable standard module width of up to 1,922 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Lightweight floor-to-ceiling door leaf coated on both sides with vinyl, varnished wood or lacquered MDF. Lock leaf with a width of 913 mm and an inactive leaf, both 100 mm or 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE X Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module X: double-glazed double door with lock leaf and inactive leaf, with stiles to ceiling. Variable standard module width of up to 1,922 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling double-glazed door leaves, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles. Lock leaf with a width of 913 mm and an inactive leaf, both 100 mm or 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE X Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module X: single-glazed double door with lock leaf and inactive leaf, with stiles to ceiling. Variable standard module width of up to 1,922 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling single-glazed door leaves, with an 8mm-thick tempered glass pane framed by painted aluminium profiles. Lock leaf with a width of 913 mm and an inactive leaf, both 100 mm or 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE X Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module X: glazed double door with lock leaf and inactive leaf, with stiles to ceiling. Variable standard module width of up to 1,922 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling tempered glazed Clarit door leaves. Lock leaf with a width of 913 mm and an inactive leaf, both 100 mm or 50 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Blind door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module Z: blind double door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Lightweight door leaves made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods and lacquered MDF panels. Door leaves are 910x2,017x100 mm or 914x2,017x50 mm. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Double-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module Z: double-glazed double door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Double-glazed door leaves, with 6mm- and 8mm-thick tempered glass panes framed by painted aluminium profiles; which are 910 mm wide, 100 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Single-glazed framed door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module Z: single-glazed double door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Single-glazed door leaves, with an 8mm-thick tempered glass pane framed by painted aluminium profiles; which are 914 mm wide, 50 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Clarit door | M2. Supply and installation of 1:10 demountable partition with hidden profiling, module Z: glazed double door with glazed fanlight. The fanlight may be double-glazed or single-glazed (centred or decentred). Standard module width: 1,923 mm. Total thickness: 100 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6060-T6 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/60 micrometres and colour tolerance per DIN 5033. 4+4, 5+5 or 6+6 mm thick panes. 60-68 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently thanks to the perimeter glass-stops on both faces. Tempered glazed Clarit door leaves; which are 914 mm wide, 10 mm thick and 2,017 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |