LINE

DEMOUNTABLE PARTITION

Descriptive memories

| ### MODULE A | M2. Supply and installation of LINE demountable partition with hidden profiling, module A: totally blind. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Acoustic insulation of 42 dB according to UNE 74040. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B | M2. Supply and installation of LINE demountable partition with hidden profiling, module B: mixed central-glass section (blind to 882 mm and glazed to 2,082 mm). Central glass section may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B blind | M2. Supply and installation of LINE demountable partition with hidden profiling, module B blind: totally blind, divided in 3 panels (grooves at 882 and 2,082 mm). Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B inverted | M2. Supply and installation of LINE demountable partition with hidden profiling, module B inverted: mixed central-blind section (glazed to 882 mm and blind to 2,082 mm). Upper and lower glass sections may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B glazed | M2. Supply and installation of LINE demountable partition with hidden profiling, module B glazed: totally glazed, divided in 3 panes (grooves at 882 and 2,082 mm). It may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE B+F | M2. Supply and installation of LINE demountable partition with hidden profiling, module B+F: mixed central and upper glass sections (blind to 882 mm and glazed to ceiling, with a groove at 2,082 mm). Central and upper glass sections may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE C | M2. Supply and installation of LINE demountable partition with hidden profiling, module C: mixed lower-glass section (glazed to 2,082 mm and blind to ceiling). Lower glass section may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE C+F | M2. Supply and installation of LINE demountable partition with hidden profiling, module C+F: totally glazed, divided in 2 panes (groove at 2,082 mm). It may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE D | M2. Supply and installation of LINE demountable partition with hidden profiling, module D: totally glazed. It may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Acoustic insulation of 46 dB in a 6+6 doubled-glazed partition, 42dB in a 5+5 doubled glazed partition and 35 dB in a 6+6 single-glazed partition according to UNE 74040. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE E | M2. Supply and installation of LINE demountable partition with hidden profiling, module E: mixed upper-glass section (blind to 882 mm and glazed to ceiling). Upper glass section may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE E blind | M2. Supply and installation of LINE demountable partition with hidden profiling, module E: totally blind, divided in 2 panels (groove at 882 mm). Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE F | M2. Supply and installation of LINE demountable partition with hidden profiling, module F: mixed upper-glass section (blind to 2,082 mm and glazed to ceiling). Upper glass section may be double-glazed or centred single-glazed. Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE F blind | M2. Supply and installation of LINE demountable partition with hidden profiling, module F blind: totally blind, divided in 2 panels (groove at 2,082 mm). Standard module width: 1,200 mm. Total thickness: 90 mm. Made with a self-supporting frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200 ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Blind door | M2. Supply and installation of LINE demountable partition with hidden profiling, module G: blind door with floor-to-ceiling door jambs. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling door leaf made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. Door leaf is 928 mm wide and 90 mm thick or 928 mm wide and 40 mm thick. Hardware: Tesa or Hoppe handle with lock in 40 mm thick door leaves and Tesa handle with lock in 90 mm thick door leaves. Acoustic insulation of 35 dB according to UNE 74040. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Double-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module G: double-glazed framed door with floor-to-ceiling door jambs. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling double-glazed door leaf, with 6 mm and 8 mm thick tempered glass panes framed by painted aluminium profiles, which is 928 mm wide and 90 mm thick. Hardware: Tesa handle with lock. Acoustic insulation of 34 dB according to UNE 74040. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Single-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module G: single-glazed framed door with floor-to-ceiling door jambs. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling single-glazed door leaf, with an 8 mm thick tempered glass pane framed by painted aluminium profiles, which is 928 mm wide and 40 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE G Clarit door | M2. Supply and installation of LINE demountable partition with hidden profiling, module G: glazed door with floor-to-ceiling door jambs. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling tempered glazed Clarit door leaf; which is 928 mm wide and 10 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Blind door | M2. Supply and installation of LINE demountable partition with hidden profiling, module K: blind door with blind top panel. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Door leaf made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. Door leaf dimensions: 928x2,041x90 mm or 928x2,041x40 mm. Hardware: Tesa or Hoppe handle with lock in 40 mm thick door leaves and Tesa handle with lock in 90 mm thick door leaves. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Double-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module K: double-glazed framed door with blind top panel. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Double-glazed door leaf, with 6 mm and 8 mm thick tempered glass panes framed by painted aluminium profiles; which is 928 mm wide, 90 mm thick and 2,041 mm high. Hardware: Tesa handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Single-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module K: single-glazed framed door with blind top panel. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Single-glazed door leaf, with an 8 mm thick tempered glass pane framed by painted aluminium profiles; which is 928 mm wide, 40 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE K ### Clarit door | M2. Supply and installation of LINE demountable partition with hidden profiling, module K: glazed door with blind top panel. Standard module width: 930 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Tempered glazed Clarit door leaf; which is 928 mm wide, 10 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Blind door | M2. Supply and installation of LINE demountable partition with hidden profiling, module P: blind door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Door leaf made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. Door leaf dimensions: 928x2,041x90 mm or 928x2,041x40 mm. Hardware: Tesa or Hoppe handle with lock in 40 mm thick door leaves and Tesa handle with lock in 90 mm thick door leaves. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Double-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module P: double-glazed framed door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Double-glazed door leaf, with 6 mm and 8 mm thick tempered glass panes framed by painted aluminium profiles; which is 928 mm wide, 90 mm thick and 2,041 mm high. Hardware: Tesa handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Single-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module P: single-glazed framed door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Single-glazed door leaf, with an 8 mm thick tempered glass pane framed by painted aluminium profiles; which is 928 mm wide, 40 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE P ### Clarit door | M2. Supply and installation of LINE demountable partition with hidden profiling, module P: glazed door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 994 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Tempered glazed Clarit door leaf; which is 928 mm wide, 10 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Blind door | M2. Supply and installation of LINE demountable partition with hidden profiling, module S: blind double door with blind top panel. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Door leaves made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. Door leaves dimensions: 930x2,041x90 mm or 930x2,041x40 mm. Hardware: Tesa or Hoppe handle with lock in 40 mm thick door leaves and Tesa handle with lock in 90 mm thick door leaves. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Double-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module S: double-glazed framed double door with blind top panel. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Double-glazed door leaves, with 6 mm and 8 mm thick tempered glass panes framed by painted aluminium profiles; which are 930 mm wide, 90 mm thick and 2,041 mm high. Hardware: Tesa handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Single-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module S: single-glazed framed double door with blind top panel. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Single-glazed door leaves, with an 8 mm thick tempered glass pane framed by painted aluminium profiles; which are 930 mm wide, 40 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE S ### Clarit door | M2. Supply and installation of LINE demountable partition with hidden profiling, module S: glazed double door with blind top panel. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. 16 mm thick particle-board panels edged and laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. The indented upper runner leaves 13 mm to the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Tempered glazed Clarit door leaves; which are 930 mm wide, 10 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Blind door | M2. Supply and installation of LINE demountable partition with hidden profiling, module W: blind double door with floor-to-ceiling door jambs. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling door leaves made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. Door leaves are 930 mm wide and 90 mm thick or 930 mm wide and 40 mm thick. Hardware: Tesa or Hoppe handle with lock in 40 mm thick door leaves and Tesa handle with lock in 90 mm thick door leaves. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Double-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module W: double-glazed framed double door with floor-to-ceiling door jambs. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling double-glazed door leaves, with 6 mm and 8 mm thick tempered glass panes framed by painted aluminium profiles, which are 930 mm wide and 90 mm thick. Hardware: Tesa handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Single-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module W: single-glazed framed double door with floor-to-ceiling door jambs. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling single-glazed door leaves, with an 8 mm thick tempered glass pane framed by painted aluminium profiles, which are 930 mm wide and 40 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE W Clarit door | M2. Supply and installation of LINE demountable partition with hidden profiling, module W: glazed double door with floor-to-ceiling door jambs. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Floor-to-ceiling tempered glazed Clarit door leaves; which are 930 mm wide and 10 mm thick. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Blind door | M2. Supply and installation of LINE demountable partition with hidden profiling, module Z: blind double door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Door leaves made in particle-board panels laminated with semi-rigid vinyl coatings. Other surface finish options include fine hardwoods or melamine and lacquered MDF panels. Door leaves dimensions: 930x2,041x90 mm or 930x2,041x40 mm. Hardware: Tesa or Hoppe handle with lock in 40 mm thick door leaves and Tesa handle with lock in 90 mm thick door leaves. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Double-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module Z: double-glazed framed double door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panels can be demounted from the frame independently. Double-glazed door leaves, with 6 mm and 8 mm thick tempered glass panes framed by painted aluminium profiles; which are 930 mm wide, 90 mm thick and 2,041 mm high. Hardware: Tesa handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Single-glazed framed door | M2. Supply and installation of LINE demountable partition with hidden profiling, module Z: single-glazed framed double door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Single-glazed door leaves, with an 8 mm thick tempered glass pane framed by painted aluminium profiles; which are 930 mm wide, 40 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### MODULE Z ### Clarit door | M2. Supply and installation of LINE demountable partition with hidden profiling, module Z: glazed double door with glazed fanlight. The fanlight may be double-glazed or centred single-glazed. Standard module width: 1,931 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and outer frame in 6063-T5 aluminium, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. The indented upper runner leaves 13 mm to the ceiling. 4+4, 5+5 or 6+6 mm thick panes. 55-65 mm gap between panes (double-glazed), depending on their thickness. The panes can be demounted from the frame independently. Tempered glazed Clarit door leaves; which are 930 mm wide, 10 mm thick and 2,041 mm high. Hardware: Tesa or Hoppe handle with lock. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |

| ### TECHNICAL MODULE | M2. Supply and installation of LINE demountable partition with hidden profiling, module A: totally blind. Standard module width: 300 mm. Total thickness: 90 mm. Made with a self-supporting inner frame in Sendzimir galvanised steel and 6063-T5 aluminium accessible covers, per EN 10.346:2009 (DX51D+Z). Previously degreased visible metal components electrostatically painted with polyester or epoxy powder and polymerised at 200ºC. Paint thickness of 50/90 micrometres and colour tolerance per DIN 5033. Painted 6063-T5 aluminium panels. There is no groove between panels. The panels close over a 2 mm thick PVC joint which provides sound insulation. Indented upper and bottom runners leave 13 mm to the floor and the ceiling. Interior insulation with 50 mm thick, 30/40 Kg/m3 dense mineral fibre. Re-installation and interchangeability of modules. Quality assurance EN ISO 9001: 2008 certified by LLOYD’S REGISTER QUALITY ASSURANCE. Includes all parts necessary for installation. Supplied and installed by manufacturer-approved distributor. |
| --- | --- |